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GC Bond 6102
Discription      :           Water based adhesive based on EVA – Copolymer.
Application
:
Side Seam adhesive for Tobacco industry up to 12000 Cig/min.
Dry Matter
:

40 – 54 %

PH-value
:

4 – 6 
Viscosity
:

350 – 950 mPa.s at 25(C acc. to





Brookfield RVT, Spdl 2/20RPM.
Storage
:

at 18-25°C.
Shelf Life
:

6 months in tightly closed package, at room tempreture.
Cleaning
:

This product can be cleaned by warm water.
Packing
:

In 25 Kg plastic jerrycan and also can be filled in plastic
                                                drums of 130kg each with PE-Inliner each drum labeled
                                                with type, batch number, net weight and expiry dates.
The information contained in this leaflet is based on our own experience. We recommend tests and adaptations to varying working conditions and materials. Our Technical service should be consulted.  We cannot accept any liability whatsoever with regard to this information.
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