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GC Bond 6103
Discription      :                       Water based adhesive based on EVA – Copolymer.
Application
:

Carton Closure adhesive for Tobacco industry

                                                speacially for the GD machines up to 500 pack/min.
Dry Matter
:

45 – 55 %

PH-value
:

4 – 6 
Viscosity
:

350 – 650 mPa.s at 25(C acc. to





Brookfield RVT, Spdl 2/20RPM.
Storage
:

at 18-25°C.
Shelf Life
:

6 months in tightly closed package, at room tempreture.
Cleaning
:

This product can be cleaned by warm water.
Packing
:

in plastic jerrycan of 25 kg each jerrycan labeled with
                                                type, batch number, net weight and expiry dates.
The information contained in this leaflet is based on our own experience. We recommend tests and adaptations to varying working conditions and materials. Our Technical service should be consulted.  We cannot accept any liability whatsoever with regard to this information.

Technical Data Sheet                    Page1                                  Issue Date: 01-11-2018


[image: image1.png][image: image2.jpg]